## Slide 1
END OF LIFE SOLUTIONS FOR BIOMATERIALS
JTI-CS2-2019-CFP10-AIR-03-07
Workshop 2nd March 2023
Nora Lardiés Miazza nlardies@aimplas.es
AIMPLAS
This project has received funding from the European Union’s Horizon 2020 research and innovation programme for the Clean SkyJoint Technology Initiative under grant agreement No 886416.
This publication reflects only the author's view and that the Commission is not responsible for any use that may be made of the information it contains.

## Slide 2
Aviation industry is increasing the biocomposite content to mitigate the environmental impact

## Slide 3
FULL SCALE DEMONSTRATION OF THE TWO MOST PROMISING EOL METHODS FOR BIOCOMPOSITE WASTE
MAIN ELIOT OBJECTIVE:

## Slide 4
They do not contain carbon fibres (whose market value is one of the primary driving forces for FRP recycling)
The technologies for their recovery have not yet been tested in depth due to the novelty of the materials

## Slide 5
WPs
Funnel methodology followed in ELIOT

## Slide 6
WPs
Funnel methodology followed in ELIOT

## Slide 7
RESULTS 1 and 2: Literature review
Composites
Biocomposites

## Slide 8
WPs
Funnel methodology followed in ELIOT

## Slide 9
RESULTS 3: MCDA and ranking of EoL strategies
MCDA overall results:
dissolution
solvolysis
Classic pyrolysis
Mechanical r.

## Slide 10
WPs
Funnel methodology followed in ELIOT

## Slide 11
Biocomposites selected to do the trials:
Flax fiber with bioepoxy matrix
Basalt fiber with PFA matrix
Carbon fiber with bioepoxy matrix
RESULTS 4: EXPERIMENTAL PROOF OF CONCEPT OF THE BEST CANDIDATES
4 technologies ranked better on circularity potential analysis and technology desirability matrix:
MECHANICAL RECYCLING
SOLVOLYSIS
DISSOLUTION
CLASSIC PYROLYSIS

## Slide 12
1) MECHANICAL RECYCLING TECHNOLOGY:
RESULTS 4: EXPERIMENTAL PROOF OF CONCEPT OF THE BEST CANDIDATES

## Slide 13
1) MECHANICAL RECYCLING TECHNOLOGY:
RESULTS 4: EXPERIMENTAL PROOF OF CONCEPT OF THE BEST CANDIDATES
Grinded biocomposites were introduced in new composites as fillers

## Slide 14
1) MECHANICAL RECYCLING TECHNOLOGY:
RESULTS 4: EXPERIMENTAL PROOF OF CONCEPT OF THE BEST CANDIDATES
CONCLUSIONS:
Mechanical properties REDUCED!
of the new biocomposites with the grinded fillers compared to the same biocomposite with a standard fillers

## Slide 15
2) PYROLYSIS:
RESULTS 4: EXPERIMENTAL PROOF OF CONCEPT OF THE BEST CANDIDATES
CONCLUSIONS:
Dry fibres and pyrolytic oils were obtained and characterized: EA, TGA, GPC, HPLC, FTIR

## Slide 16
2) PYROLYSIS: characterization of the pyrolytic oils collected after the pyrolysis
Examples of chromatograms (HPLC-GPC with UV detector):
RESULTS 4: EXPERIMENTAL PROOF OF CONCEPT OF THE BEST CANDIDATES

## Slide 17
3) SOLVOLYSIS:
RESULTS 4: EXPERIMENTAL PROOF OF CONCEPT OF THE BEST CANDIDATES
Solvents, catalysers, temperature and pressure
Monomers Recovery
Fibres recuperation

## Slide 18
3) SOLVOLYSIS:
RESULTS 4: EXPERIMENTAL PROOF OF CONCEPT OF THE BEST CANDIDATES
CONCLUSIONS:
Good quality of the dry fibres and a mixture of products was obtained from the organic residue

## Slide 19
4) DISSOLUTION TECHNOLOGY:
RESULTS 4: EXPERIMENTAL PROOF OF CONCEPT OF THE BEST CANDIDATES
CONCLUSIONS:
Broad range of solvent classes was tested but:
no suitable solvent (and dissolution conditions) were found for any of the studied materials

## Slide 20
WPs
Funnel methodology followed in ELIOT

## Slide 21
BEST TECHNOLOGIES SELECTED FROM WP5 TO MAKE THE PILOT PLANT SCALABILITY
PYROLYSIS AND SOLVOLYSIS:
RESULTS 5: EVALUATION OF FULL-SCALE DEMONSTRATOR AND LCA DATA COLLECTION
CONLUSIONS:
Regarding PYROLYSIS
8 mm and 20 mm grinded biocomposites were pyrolyzed
More residue than in WP5 are obtained over the surface of the fibres making compulsory an afterwards oxidation step to eliminate it
The PFA resin is easier to pyrolyzed than the bioepoxy resin
Phenol is the most abundant and valuable product obtained in the liquid’s parts from the pyrolysis

## Slide 22
BEST TECHNOLOGIES SELECTED FROM WP5 TO MAKE THE PILOT PLANT SCALABILITY PYROLYSIS AND SOLVOLYSIS:
RESULTS 5: EVALUATION OF FULL-SCALE DEMONSTRATOR AND LCA DATA COLLECTION
CONLUSIONS:
2) Regarding SOLVOLYSIS
8 m and 150x150 mm plates were solvolysed
Solvolysis performed even better when the size of the initial biocomposite is high (as high as the size of the reactor feeding point)
The organic residue obtained after the distillation of the solvents still contains reagents from the solvolysis reaction
In both cases pyrolysis and solvolysis further purification steps are compulsory to take advantage of the liquid/wax part and the organic residue from pyrolysis and solvolysis respectively
Notes: This opens the door to industrial solvolysis processes with big reactors to maximize the length of the fibres recycled obtained.

## Slide 23
FULL LIFE CYCLE ASSESMENT results:
RESULTS 5: EVALUATION OF FULL-SCALE DEMONSTRATOR AND LCA DATA COLLECTION
Solvolysis performs the best
Pyrolysis emits 17% more carbon dioxide than solvolysis
Regarding the heat input pyrolysis consumes approximately twice as much heat as solvolysis
Additional heat in pyrolysis, is in solvolysis substituted with solvents, which are recovered with high efficiency and reused in the process
Notes: for 1 kg of basalt-bioPFA composite

## Slide 24
FULL TECHNO-ECONOMIC ASSESSMENT results:
RESULTS 5: EVALUATION OF FULL-SCALE DEMONSTRATOR AND LCA DATA COLLECTION
Both investigated technologies are compared in terms of different indicators of TEA (Techno-Economic Assessment)
The estimates are based on a processing plant with a capacity of 10 kilotonnes of biocomposite per annum
The comparison of the results show a higher cost for heat for pyrolysis
Solvolysis is associated with higher costs for capital investment noting the costs associated with the equipment
Notes: which can be explained by the significant heating energy requirements of the process

## Slide 25
ELIOT TEAM:
Thank you for your attention!
Nora Lardiés Miazza
Chemical recycling area
nlardies@aimplas.es
Sergio Fita Bravo
Project manager
sfita@aimplas.es
Pouya Samani pouya.samani@tno.nl
Spela Ferjan spela.ferjan@tno.nl
Clare Harvey lare.harvey@tno.nl
Milkica Jovicic milkica.jovicic@tno.nl
https://project-eliot.eu